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A separate internal moulding to take the floorboards shall be bonded to the exterior hull moulding and it shall extend at least from station 3 to station 12.
The top edge of the moulding shall not be below a continuous fair curve on each side of the yacht between the minimum points. No part of the moulding shall extend below 1000mm from a line joining the two sheerlines nor shall it, at any point, extend higher than 200mm below the deck.
The internal moulding may incorporate a web or frames, at its forward and aft ends.
The weight of the laminate in the internal moulding shall be not less than 8.1kg/m.
Example of construction:
	Gelcoat
	0.60 kg/m

	5 layers of 450g/m glass   thickness 4mm
	7.50 kg/m

	
	

	Total
	8.10 kg/m


Horizontal surfaces shall be of sandwich construction with no less than 10mm closed cell foam or balsa of not less than 60 kg/m between the third and fourth layer of glass.
The internal moulding shall be bedded on a uniform wet laminate of not less than 3kg/m or may be bonded within the weight requirements of rule 2.403.
The space below the cockpit shall be filled with closed cell foam or balsa in accordance with the drawings.
Floors in not less than 10 layers of 450g glass mat per m², in a thickness of 8mm, and forming a Z, shall be fitted in accordance with rule 2.407. 
The internal moulding can in section no. 11 be constructively integrated with the forward berth. According to the principle shown on drawing GRP 6 Longitudinal arrangements. The weight of the laminate in the forward berth shall be not less than 8.1kg/m². 
A small bulkhead along the sides of the hull to separate the forepeak and main cabin are allowed, but the opening area between the spaces (cabin and forepeak) shall not be less than 0.55 m2. The minimum opening area 0,55m2 is in one piece. It is not permitted to divide the opening area into several parts.

The bulkhead shall consist of: Wood not less than 12 mm and not more than 16 mm thickness, not exceeding 800 kg/m3. Or be of a GRP (glass reinforced polyester) sandwich construction. The core shall be in closed cell foam or balsa. The total weight of the bulkhead in a sandwich construction shall be not more than 8,1 kg/m.

Example of a bulkhead in sandwich construction:
	2 layers resin coat
	0,6 kg/m

	2 layers of 450g/m glass and resin
	2.7 kg/m

	15mm closed cell foam of 60kg/m
	0.9 kg/m

	Resin for foam
	0.4 kg/m

	2 layers of 450g/m glass and resin
	2.7 kg/m

	2 layers resin coat
	0,6 kg/m

	
	

	Total
	7,9 kg/m




